Conversion for dissolving KOH and NaOH:

Process for embedding filter in a urethane substrate:

- Place double-sided sticky tape (thin scotch tape) on a plastic film

- Firmly press the filter onto the sticky tape

- Properly mix the desired urethane hardener and resin in a beaker

- Degas the mixture

- Pour the urethane on the plastic film on the filter

- Degas the poured urethane

- Let the urethane cure

- After the urethane is cured, peel the urethane off the plastic and peel the tape off the urethane

Process for dissolving a filter embedded in a urethane substrate:

- Mix 5g KOH with 90g H2O to form a 1 molar solution of KOH in a glass beaker

  - Wear gloves

  - Measure the appropriate amount of KOH

  - Pour hot water in the beaker

  - Pour the KOH in the hot water

  - Mix the solution with a stirring rod

Note: KOH absorbs moisture quickly so be sure to quickly reseal the stock KOH.  Wear gloves - KOH is caustic and will burn the skin and eye.

- Placed urethane substrate in solution.

- Waited 12 hrs.

- Removed substrate from solution, and rinsed with water

- The KOH solution does not need special disposal because of its low concentration.  Pour it in the sink.